## Slide 1
Physical Properties
Test parameter | VIXUM® IWN | VIXUM® AGN / IGN | Test Method
Color | White | Light Gray / Dark Gray | -
Size (㎜) | 1250 × 2560 × 380 | 1260 × 2560 × 380 | 1.0 CBM
Density (kg/m3) | 9.5 ± 1.5 | 9.5 ± 1.5 | ISO 845
Hardness (F0 type) | Ave. ≥ 60 | Ave. ≥ 60 | -
Tensile Strength (KPa) | Ave. ≥ 100 | Ave. ≥ 100 | ISO 1798
Elongation (%) | Ave. ≥ 15 | Ave. ≥ 15 | ISO 1798
Hazardous Substances / Formaldehyde Emission | Class Ⅱ Pass Max. ≤ 75mg/kg Pass Pass | Class Ⅱ Pass Max. ≤ 75mg/kg Pass Pass | OEKO-TEX 100 (Europe) REACH SVHC (as of 180627) ISO 14184-1 (Water Extraction) ISO 16000-9 (CA 01350/USA) EN 717-1 (Europe)
Fire Behavior | V-0 Class A FSV 0 / SDV 15 - - | V-0 Class A FSV 0 / SDV 18 B-s1d0 Class B1 | UL-94 ASTM E84-16 (USA) CAN/ULC-S102 (Canada) EN 13501-1 (Europe) DIN 4102-1 (Germany)
Sound Absorption Coefficient (50㎜) | NRC ≥ 0.85 | NRC ≥ 0.85 | ISO 354
Thermal Conductivity (W/m·K) | Max. ≤ 0.035 | Max. ≤ 0.035 | KS L 9016
Certification for Train | - | HL3 S-4, ST-2, SR-2, Pass | EN 45545-2 (Europe) DIN 5510-2 (Germany)
19, Hasinbeonyeong-ro, Saha-gu, Busan, Republic of korea 49470
http://www.vixum.co.kr
IWN
AGN
IGN
Page 2

## Slide 2
Sound Absorption as per thickness range
Chart: 1/3 Octaveband Center Frequency(Hz)
| 100 | 125 | 160 | 200 | 250 | 315 | 400 | 500 | 630 | 800 | 1000 | 1250 | 1600 | 2000 | 2500 | 3150 | 4000 | 5000
10mm | 0.04 | 0.03 | 0.07 | 0.06 | 0.1 | 0.13 | 0.17 | 0.23 | 0.29 | 0.39 | 0.41 | 0.51 | 0.59 | 0.65 | 0.66 | 0.72 | 0.73 | 0.74
25mm | 0.06 | 0.04 | 0.06 | 0.14 | 0.16 | 0.23 | 0.31 | 0.4 | 0.52 | 0.63 | 0.69 | 0.8 | 0.85 | 0.91 | 0.9 | 0.92 | 0.93 | 0.95
50mm | 0.08 | 0.1 | 0.16 | 0.31 | 0.42 | 0.57 | 0.71 | 0.88 | 0.94 | 1.04 | 1.06 | 1.09 | 1.07 | 1.06 | 1.07 | 1.07 | 1.09 | 1.12
100mm | 0.24 | 0.24 | 0.45 | 0.73 | 0.95 | 1.11 | 1.19 | 1.17 | 1.2 | 1.22 | 1.19 | 1.17 | 1.13 | 1.15 | 1.13 | 1.12 | 1.14 | 1.17
Sound Absorption Test as per ISO 354
NRC : Noise Reduction Coefficient(250Hz, 500Hz, 1000Hz, 2000Hz)
 | VIXUM(10mm) | VIXUM(25mm) | VIXUM(50mm) | VIXUM(100mm)
NRC | 0.35 | 0.54 | 0.86 | 1.10
Thermal Conductivity as per temperature range
Chart: Temperature(℃)
| -10℃ | 0℃ | 20℃ | 40℃ | 60℃ | 80℃ | 100℃ | 120℃ | 140℃ | 160℃ | 180℃ | 200℃ | 210℃
 | 0.029 | 0.03 | 0.033 | 0.037 | 0.04 | 0.037 | 0.04 | 0.043 | 0.045 | 0.047 | 0.051 | 0.056 | 0.056
19, Hasinbeonyeong-ro, Saha-gu, Busan, Republic of korea 49470
http://www.vixum.co.kr
Page 3

## Slide 3
Heat resistance
Chart: Time(hr)
| 0 | 500 | 1000 | 1500 | 2000
 | 100 | 73 | 60 | 53 | 46
Test Temperature : 190 ± 2℃
Tensile Strength was measured as per ISO 1798
Comparison with other materials
 | PET | PP | PU | Glass Wool | VIXUM
Base Material | Polyester | Polypropylene + Polyester | Polyurethane | SiO2 | Melamine
Thermal Conductivity(W/m·K) | ≤ 0.036 | ≤ 0.037 | ≤ 0.027 | ≤ 0.037 | ≤ 0.035
Density(kg/m3) | 13 ~ 32 | 14 ~ 62 | 16 ~ 30 | 100 ~ 160 | 8 ~ 11
Heat Resistance | ＜ 70℃ | ＜ 70℃ | ＜ 100℃ | ＜ 350℃ | ＜ 240℃
Fire Resistance | Poor | Poor | Poor | Excellent | Good
Thermoforming | Poor | Poor | Good | Poor | Good
19, Hasinbeonyeong-ro, Saha-gu, Busan, Republic of korea 49470
http://www.vixum.co.kr
Page 4